## Slide 1: Perovskite nanoparticles
Synthesis and optical properties

## Slide 2: Perovskite structure

## Slide 3: Hot injection method
nanoparticles size control
monodisperse
special conditions
high temperature

## Slide 4: Alternative synthesis methods
simplicity
room temperature
polydispersity
uncontrolled NPs size and structure
Ultrasonic method
Antisolvent method

## Slide 5: Perovskite structure
Sample | Point group | a, Å | β, ⁰ | Crystal size, nm
CsPbBr3 | Pm-3m | 5.81 | 90 | 27.6 ± 5.2
CsPbCl3-zBrz | Pm-3m | 5.80 | 90 | 33.4 ± 8.9
CsPbCl3 | Pm-3m | 5.69 | 90 | 14.5 ± 1.3
CsPb1-yMnyCl3-zBrz | Pm-3m | 5.69 | 90 | 17.1 ± 2.4
CsPb1-yMnyCl3 | Pm-3m | 5.57 | 90 | 20.7 ± 3.9

## Slide 6: NPs size, shape and the ratio of elements
Sample |  | Theoretical atomic ratio | Experimental atomic ratio
CsPbBr3 |  | СsPbBr3 | CsPb1.2Br2.5
CsPbCl3-zBrz |  | CsPbCl1.5Br1.5 | Cs1.1PbCl0.59Br2.59
CsPbCl3 |  | CsPbCl3 | CsPb1.3Cl1.3
CsPb1-yMnyCl3-zBrz |  | CsPb0.3Mn0.7Cl2.5Br0.5 | CsPb1.2Mn0.7Cl2.5Br2.2
CsPb1-yMnyCl3 |  | CsPb0.3Mn0.7Cl3 | CsPb0.8Mn0.7Cl2,58

## Slide 7: Optical properties
Emission spectra
Absorption spectra

## Slide 8: Size control
Emission spectra

## Slide 9: CsPbBr3 and Cs4PbBr6 perovskite
CsPbBr3. Hot injection synthesis.
Cs4PbBr6. Ultrasonic method of synthesis.

## Slide 10: CsPbBr3 and Cs4PbBr6 perovskite

## Slide 11: CsPbBr3 and Cs4PbBr6 perovskite

## Slide 12: Alternative synthesis methods. Optical properties
Absorption and emission spectra
NPs layer structure
Antisolvent method of synthesis